## Slide 1: Weekly Report 10/24/22
Erin Ingram & Omar Mahmood
NanoBio Systems Lab
Texas A&M University

## Slide 2: Progress
COMSOL simulations for electric field strength/height between IDE fingers of varying width and distance (see following slides)
Cleanroom training – preparing for IDE fabrication, for our own device
  Applied positive/negative resists to gold plate/silicon wafer
    Used spin coater to reduce thickness of resist layer
  Photolithography using EVG 610 on gold plate using IDE mask
    Cleaned off remaining resist, checked IDE pattern under microscope
Application of positive resist to gold plate in spin coater
IDE mask

## Slide 3: Electric field simulation
Finger width: 5um
Finger distance: 5um

## Slide 4: Electric field simulation
Finger width: 10um
Finger distance: 10um

## Slide 5: Electric field simulation
Finger width: 20um
Finger distance: 20um

## Slide 6: Goals for next week
Continue cleanroom training and IDE fabrication
  Wet etching
  Metal deposition

## Slide 7: Thank you for your time!